## Slide 1: Comparative Life Cycle Assessment of Aluminium and Carbon Fiber Bike Frames
Lazy Caffeine Addicts:
Aanand Nataraj Satheesh Manimala
Alessandro Gorla
Áron Zsombor Sebó
Malte Pelle Rietdorf

## Slide 2: Background and Methodology
Specialized-Allez Sprint​ | Specialized-Tarmac SL7​
Aluminum​ | Carbon Fiber​
2.35kg​ | 0.8kg​
Goal: Find frame with least amount of environmental impact
Comparison of Energy usage and CO2 emissions
Data: from Reports, and Tools (Gabi…)
System boundaries:
Lazy Caffeine Addicts
Notes: 1-2 min
Motivation and Goal
System boundary
Data collection: what (Energy usage and CO2 emissions) and how (reports, tools (Gabi,…)

## Slide 3: LCA of Aluminium Bike Frame
CO2 eq emission displaced by recycling aluminum will be considered.
 | Energy Consumption​ | CO2 Emissions | 
Extrusion | ​7.36 MJ/Kg | 6.57 kg CO2 eq / ton | 
Tube Hydroforming | 75.6 MJ/Kg | Yet to collect / data unavailable | 
Miter Cuts | 178.5 KJ/Cut | 0.0426 Kg CO2 eq / cut | 
TIG Weld | 38.3 MJ/metre | 2.44 Kg CO2 eq/ metre | 
T6 Heat treatment | Yet to collect / Data unavailable |  | 
Painting | ~10 MJ / bike |  | ~5 kgCO2 / bike
 | Energy Consumption​ | CO2 Emissions
Cutting | ​0.04 MJ / Cut | Yet to collect / Data unavailable
Recycling | 34 MJ/Kg | Yet to collect / Data unavailable
Aluminium | Energy Consumption​ | CO2 Emissions
Raw Material Extraction | ​157207 MJ/ton | 15947 kg CO2 eq / ton
Transportation | 0.209 MJ/ton/km | 32.8 CO2 eq/km/ton
Lazy Caffeine Addicts
Considerations:
Bike frame made with Virgin Aluminium
Aluminium Ingots are produced in China and transported to Europe through ocean(13000 kms)
Transportation from the shipyard to the factory in Germany is also modelled through rail transportation (630 kms)
Raw-Material Extraction phase
Considerations
Total Wastage from Manufacturing operations is considered as 10% of the input material for producing one bike
  Weight of the end product- 2.35 Kg. Input material considering wastage- 2.6 Kg
  Total number of Miter cuts after hydroforming tubes = 16 for each bike frame
  Total number of Welded joints = 11 for each frame
    Average tube diameter= 50 mm total weld length=1.7 m
Manufacturing phase
Recycling Phase
Frames are cut to reduce size for easy handling for recycling, this energy is considered.
Transportation is ignored due to high complexity of logistics.
Notes: as bikes may travel varying distances based on local recycling infrastructures, collection methods, and market demands for recycled materials

## Slide 4: LCA of Carbon Fiber
Carbon fiber | Energy Consumption​ (MJ/bike) | CO2 Emissions (kgCO2 eq/bike)
Raw Materials | ​550.94 | 74.29
Frame Production | 46.75 | 6.53
Transportation(s) | 2.07 | 209.53
End of Life (average of multiple scenarios) | 12.00 | 1.47
Total: | 611.77 | 291.83
Frame made from CF prepreg
Mold made out of 100% recycled aluminium
Frame sold separately, not assembled in factory
Calculated with manufacturing losses (prepreg cutting, postprocessing, painting)
Transport by rail and ferry, same as before
Production locations based on real suppliers
Lazy Caffeine Addicts
Process | Location
Resin, Fiber | Japan
Prepreg production | Japan
Paint | China
Recycled Aluminium | China
Frame production | Taiwan
Postprocessing, painting | Taiwan
Warehouse | Netherlands
Notes: Max. 3 minutes!
Flowchart production
Flowchart transportation
Table with Energy consumption and CO2 emissions
Different EoL recycling methods

## Slide 5: Next Steps to Finish the Report?
Collect missing data and finish calculations
1
Aluminium: compare both scenarios (virgin and recycled Al)
2
Carbon Fiber: Compare recycling methods
3
Compare both materials
4
Final Discussion
5
Lazy Caffeine Addicts
Notes: 1-2 minutes